## Slide 1
Tunable Nano-Photonic Devices
Susobhan Das

## Slide 2
  Graphene
    Experimental Setup
    Result and Discussion
  Indium Tin Oxide
  Vanadium di-Oxide
    Transmission Characteristics
    Experimental Setup
    Result and discussion
  NIR Electro Optic Modulator based on Graphene
  Mode-Multiplexed Modulator
  Metamaterial Assisted Coupler
Optical Devices
Material Characterization
Conclusion
Future work
Outline
Motivation
  Exploration of novel photonic structures based on surface plasmonics
  Metamaerial assisted optical devices
  Tunability in Terahertz region with patterned Graphene configuration

## Slide 3
Motivation
Photonic Integration  Compactness, high efficiency
Need for optical interconnects
Building Blocks : waveguide, modulator, coupler, router, switch, detector.
Integration  High Bandwidth, speed enhancement, Low Loss, Functionality per Area , Cost Effective, Immune to EMI
Photonic circuit based on silicon technology , its deficiency (electro optic properties) and limitation of device size by diffraction limit.
M. J. Kobrinsky et al., Intel Technol. J., 8, 2004.
Contd.

## Slide 4
Plasmonic effect  metal dielectric interface ( Au, Ag  very high negative permittivity)
New material in NIR region Graphene, ITO, VO2
New photonic device development with plasmonic effect.
P. G. Etchegoin et al. J. Chem. Phys. 127, 164705

## Slide 5
Total Internal Reflection (ncore > nclad)
d
ncore
nclad
nclad
Phase change due to TIR
Optical Waveguide
Ridge Waveguide
Optical fiber
Planar Waveguide
Fundamental Mode profile
K. Okamoto, Fundamental of Optical Waveguides (2nd eddition), Academic Press, 2006
Device size limited by diffraction limit !!!
A C

## Slide 6: Silica glass nanowaveguides
HE11x
x

## Slide 7
plasmons are collective oscillations of the free electron as density.
Surface Plasmon polariton: coupling between the EM wave & free electron movement on the metal surface.
Surface plasmon polaritons only exist for TM polarization.
The Drude Model
N free electron concentration
Polarization =
e  electronic charge ;
me the effective mass of free electrons;
Г  damping Coefficient ;
E amplitude of the incident electric field
ωfrequency of incident field
S. A. Maier, Plasmonics : Fundamentals and applications , Springer, 2007
Surface Plasmon
Confine electromagnetic field below diffraction limit
Metal
Dielectric

## Slide 8
Major Goals
Miniaturization of Devices
Tunable Device
Optical Interconnects at Telecom Wavelength
Problems
Diffraction Limit
Poor EO of Si
Solutions
Graphene

## Slide 9
Intraband Contribution
Interband Contribution
Fermi velocity
p-doped
n-doped
Fermi level
Energy (E)
Momentum (k)
Chemical Potential
Fermi-Dirac distribution
Chemical Potential
=0.34 nm, thickness of mono layer graphene
Kubo’s formula
eox dielectric constant
dox thickness of SiO2 layer
VD Dirac voltage
G. W. Hanson, J. Appl. Phys, 103, 064302.
Energy Band Diagram of Graphene
V-Vdirc
Chemical Potential (eV)
eox
dox
V

## Slide 10
Experimental Setup for Graphene Characterization
nox
ns
dox=95 nm
V

## Slide 11
Result and Discussion
nox
ns
dox

## Slide 12
Major Goals
Miniaturization of Devices
Tunable Device
Optical Interconnects at Telecom Wavelength
Problems
Diffraction Limit
Poor EO of Si
Solutions
Graphene
Other Material
Vanadium di-Oxide
Field Enhancement

## Slide 13
Kim, H., et al., Applied Physics Letters, 104, 081913
Transmission Characteristics

## Slide 14
WDM: Wavelength division multiplexer/demultiplexer between 1530nm and 1550nm.
EOM: electro-optic modulator,
EDFA: erbium-doped optical amplifier,
RFA: radio frequency amplifier
Experimental Setup for Vanadium di-Oxide

## Slide 15
d = 200nm
nm = 1.977+j2.53
ns = 3.243+j0.346
Result and Discussion
Notes: Recovery time

## Slide 16
Major Goals
Miniaturization of Devices
Tunable Device
Optical Interconnects at Telecom Wavelength
Problems
Diffraction Limit
Poor EO of Si
Solutions
Graphene
Vanadium dioxide
Solutions  Plasmonics
Problem  Too high er NIR (Au/Ag)
Solution  ITO
Field Enhancement

## Slide 17
/m3, with modeling parameters
eV
THz
Indium Tin Oxide
E. Feignbaum, K. Diest, and H. A. Atwater, Nano Letters, 10, 2111.

## Slide 18
Major Goals
Miniaturization of Devices
Tunable Device
Optical Interconnects at Telecom Wavelength
Problems
Poor EO of Si
Solutions
Graphene
Vanadium dioxide
Optical Devices
  NIR Electro Optic Modulator based on Graphene
Diffraction Limit
Solutions  Plasmonics
Problem  Too high er NIR (Au/Ag)
Solution  ITO
Field Enhancement

## Slide 19
C. T. Phare, ,et al, Nat. Photonics, 9,2015
M. Liu, et. al. Nat. 474,64-67( 2011)
H. Dalir, ,et al, ACS . Photonics, 3,2016
Review of ongoing trend

## Slide 20
Graphene -waveguide
at 1550 nm
0eV
0.5eV

## Slide 21
Schematic Diagram
Mode Profile
420 nm x 300nm
10nm HfO2
Separation between ITO bars = 10nm

## Slide 22
Optimization
Performance

## Slide 23
Major Goals
Miniaturization of Devices
Tunable Device
Optical Interconnects at Telecom Wavelength
Problems
Diffraction Limit
Poor EO of Si
Solutions
Graphene
Vanadium dioxide
Optical Devices
  NIR Electro Optic Modulator based on Graphene
  Mode-Multiplexed Modulator
Solutions  Plasmonics
Problem  Too high er NIR (Au/Ag)
Solution  ITO

## Slide 24
Electric displacement
D1=D2
ε1 E1 = ε2 E2
D2
D1
ε1
ε2
ITO
ENZ- field enhancement

## Slide 25
H. Zhao, et. al., IEEE JSTQE, 21 (4), PP. 3300207 (2015).
A. Melikyan, et. al. Optics Express, 19 (9), 8855-8869 (2011).
V. J. Sorger, et. al., Nanophotonics. 1 (1),17–22 (2012).
Review of ongoing trend

## Slide 26
Modal Dichroism
Mode 1
Mode 2
Only TE Mode
Spatially Localized Absorption Mechanism
Max with Min

## Slide 27
Schematic Diagram and Mode profile
800 nm x 240nm
20nm SiO2
ITO bars
thickness= 10nm
ITO under Potential
Accumulated electron concentration
Space dependent permittivity

## Slide 28
Modulation Scheme
Field Distribution

## Slide 29
Major Goals
Miniaturization of Devices
Tunable Device
Optical Interconnects at Telecom Wavelength
Problems
Diffraction Limit
Poor EO of Si
Solutions
Graphene
Vanadium dioxide
Solutions  Plasmonics
Problem  Too high er NIR (Au/Ag)
Solution  ITO
Optical Devices
  NIR Electro Optic Modulator based on Graphene
  Mode-Multiplexed Modulator
  Metamaterial Assisted Coupler

## Slide 30
Complex Media
Review of ongoing trend
J. B. Pendry et.. al. Science , 3121, 780 (2006)
A. Salandrino, N. Engheta, PRB, 74, 075103 (2006)

## Slide 31
Tunable Metamaterial
Schematic of Coupler
Graphene permittivity
at 1550 nm
Periodicity: 3nm
HfO2/Graphene

## Slide 32
Coupling Scheme
Field Distribution

## Slide 33
  Graphene
    Experimental Setup
    Result and Discussion
  Indium Tin Oxide
  Vanadium di-Oxide
    Transmission Characteristics
    Experimental Setup
    Result and discussion
  NIR Electro Optic Modulator based on Graphene
  Mode-Multiplexed Modulator
  Metamaterial Assisted Coupler
Optical Devices
Material Characterization
Conclusion
Future work
  Exploration of novel photonic structures based on surface plasmonics
  Metamaerial assisted optical devices
  Tunability in Terahertz region with patterned Graphene configuration
Outline

## Slide 34
Conclusion
  Metamaterial Assisted Coupler
Tunability of graphene with applied external voltage
DMT of VO2 and optical short pulse conversion
  NIR Electro Optic Modulator based on Graphene
  Mode-Multiplexed Modulator

## Slide 35
  Graphene
    Experimental Setup
    Result and Discussion
  Indium Tin Oxide
  Vanadium di-Oxide
    Transmission Characteristics
    Experimental Setup
    Result and discussion
  NIR Electro Optic Modulator based on Graphene
  Mode-Multiplexed Modulator
  Metamaterial Assisted Coupler
Optical Devices
Material Characterization
Conclusion
Future work
  Exploration of novel photonic structures based on surface plasmonics
  Metamaerial assisted optical devices
  Tunability in Terahertz region with patterned Graphene configuration
Outline

## Slide 36
Future Work
  Exploration of novel photonic structures based on surface plasmonics
  Metamaerial assisted optical devices
  Tunability in Terahertz region with patterned Graphene configuration

## Slide 37
Publication
JOURNAL ARTICLES
R. Goul, S. Das, Q. Liu, et al, “Quantitative analysis of surface enhanced Raman spectroscopy of Rhodamine 6G using a composite graphene and plasmonic Au nanoparticle substrate” Carbon, Vol. 111, pp. 386-392, 2017
S. Das, S. Fardad, I. Kim, J. Rho, R. Hui, and A. salandrino, “ Nanophotonic Modal Dichroism: Mode-Multiplexed Modulators Optics Letters, Vol. 41, No. 18, pp. 4394-4397, 2016.
S. Fardad, S. Das, A. salandrino, E. Breckenfeld, H Kim, J. wu, and R. Hui1,”All-optical short pulse translation through cross-phase modulation in a VO2 thin film” , Optics Letters, Vol. 41, No. 2, pp. 238-241, 2016.
X. Wang, S. Fardad, S. Das, A. Salandrino, and R. Hui, “Direct Observation of Bulk Second Harmonic Generation inside a Glass Slide with Tightly Focused Optical Fields” Physical Review B 93, 161109(R), 2016
S. Das, A. Salandrino, J. Z. Wu,and R. Hui,”Near-infrared electro-optic modulator based on plasmonic graphene” Optics letters ,Vol. 40, No. 7 , pp. 1516-1519, 2015.
F. Xu, S. Das, Y. Gong, Q. Liu, H. C. Chien, H. Y. Chiu, et al., "Complex refractive index tunability of graphene at 1550 nm wavelength," Applied Physics Letters, vol. 106, p. 031109, 2015.
S.Das, J. Li and R. Hui, “Simulation of the Impact of Si Shell Thickness on the Performance of Si-Coated Vertically Aligned Carbon Nanofiber as Li-Ion Battery Anode” Nanomaterials, Vol. 5, pp. 2268-2278, 2015.
CONFERENCES PRESENTATIONS
S.Das, J. Li and R. Hui, “Impact of Electrode Surface/Volume Ratio on Li-ion Battery Performance” the Proceedings of the 2014 COMSOL Conference in Boston.